# Mid-Point Check-in: AI for Science & Engineering

Project title: Physics-guided, evidence-first polymer property prediction from repeat-unit SMILES
Team name: Sandman (confirm official spelling before export)
Primary domain: Materials science / polymer informatics
Submission metric: unweighted mean of seven target-wise R² values.

This check-in reports a seven-property pipeline for glass-transition temperature (Tg), chain and bulk bandgaps (Egc, Egb), ionisation energy (Ei), electron affinity (Eea), refractive index (n), and dielectric constant (ε). The submitted notebook records a 0.907551 mean R² on the local held-out verification panel and 0.920 on the public leaderboard. The public score is reported only as a submitted-system outcome; architecture choices are made with structure-aware validation, not leaderboard feedback.

## 1. Proposed Strategy & Technical Novelty

### AI methodology and the reason for it

This is not one pooled regression task. Every target receives the same one-seventh weight although its data volume, physical mechanism, and interpolation support differ sharply. An unnormalised joint loss would therefore over-prioritise Tg, whose variance dominates the table. We instead use one shared chemistry representation and seven target-specific prediction lanes.

Figure 1. The architecture is deliberately hybrid. Classical trees and kernels are strong small-tabular baselines; a GINE graph network is retained only as a decorrelated second opinion, not as a universal replacement. Out-of-fold non-negative least-squares blending limits cancellation-based overfitting.

| Design element | What it captures | Why it is retained |
| --- | --- | --- |
| RDKit descriptors + Morgan counts | bulk chemistry plus local functional motifs | complementary signals for a limited-label regime |
| Polymer-specific atomic triples + label-free corpus SVD | local polymer chemistry and unlabelled structural context | retained only when grouped validation improves |
| Target-specific trees, kernels and compact neural arm | different sample sizes and error modes | avoids pretending all seven properties have one mechanism |
| Guarded relations: Egc≈Ei−Eea, Egb from Egc, ε=n²+ionic | known structure between co-measured properties | a route fires only with a legitimate training-label partner and cannot worsen the validated learned estimate |
| Applicability tier + interval | similarity-aware boundary of use | a user sees the evidence context, not just a point prediction |

The central novelty is evidence-first physics guidance: a physical relation is not included because it is plausible; it must improve a held-out route. For example, a learned residual on the Egc=Ei−Eea identity worsened low-data leave-one-out behaviour, so the residual was rejected. The ε decomposition is used because the ionic contribution was non-negative on the audited co-measured subset. This separates a scientific constraint from decorative “physics-informed” wording.

### Featurisation and SMILES invariance

RDKit-canonical graph features anchor the representation. The character n-gram arm is deliberately a small residual component because different valid SMILES strings can represent the same polymer. We stress-test random valid SMILES rewrites rather than merely asserting invariance: the recorded graph-derived path has zero 1σ violations across all seven targets and a worst target standard deviation of 0.230% of its training-standard-deviation scale. Attribution stability is also tested, because equal scalar predictions with different reasons would not be trustworthy.

## 2. Preliminary Salient Results

### EDA finding that changed the model

There are no exact polymer–property pairs shared between train and evaluation for six targets, yet many DFT-evaluation structures have a different measured property in training; Tg is far closer to true structure-to-property extrapolation. This makes grouped structural validation and guarded cross-property routes necessary. It also explains why a single “best model” is not defensible for all targets.

Current quantitative result. The recorded local held-out panel has per-target R² values from 0.871 (Ei) to 0.927 (Egb), with mean 0.902509 for the compact verification model. The final submitted notebook outcome is 0.907551; its per-target parity plot is intentionally deferred until the pinned isolated rerun has completed, so the report does not claim a figure from an unverified intermediate artefact.

Figure 2. Evidence beyond the leaderboard. (a) graph-feature prediction invariance under valid SMILES rewrites; (b) explanation stability across the same rewrites (mean cosine 0.980); (c) mean R² under canonical-group (0.824) and scaffold (0.660) splits; and (d) the useful robustness boundary—Tg error rises from 14.8 to 43.6 °C as nearest-training similarity falls. Figure script and source tables are listed in Appendix B.

### Explainability for future materials discovery

For electronic discovery (Egc, Egb, Ei, Eea), the model exposes which conjugation-adjacent, ring, and band-edge features support a prediction, while the Egc/Ei/Eea relationship provides a consistency check. For optical discovery (n, ε), explanation is split into the optical n² channel and the ionic/polar channel, so a proposed repeat unit can be discussed in terms of polarisation mechanisms rather than a generic importance score. Tree explanations are tested by feature-removal intervention: on the Tg proxy, masking the top 10% SHAP-ranked features produced a 0.851 R² loss versus 0.043 under an equal random mask. This supports predictive fidelity in the stated feature space, not a claim of chemical causality.

## 3. Technical Challenges & Pivots

| Challenge | Evidence-led pivot |
| --- | --- |
| Small electronic/optical tables make flexible models unstable | use target-specific classical/compact models, grouped folds, and conservative blending rather than a monolithic deep model |
| A single high score can hide unfamiliar-chemistry failure | add a structural generalisation ladder, nearest-neighbour similarity, and an applicability tier |
| SMILES text is non-unique | make graph/canonical features the invariance backbone; isolate and test the string residual separately |
| Plausible explanations can be unstable or non-load-bearing | report feature-removal fidelity and rewrite-stability; retain cross-model rank agreement (ρ=0.472 vs pre-set 0.60 bar) as a limitation |
| Archive uncertainty artifacts disagree | do not present conformal-coverage or error–uncertainty-correlation as a success until the isolated rerun regenerates one authoritative table |

The last row is an intentional transparency decision. Existing archived tables disagree on two uncertainty summaries. Rather than select a favourable number, the final release is gated on a fresh pinned run. The currently verified robustness claim is the monotone similarity–error relationship and the explicit domain warning; strict interval calibration remains in refinement.

## 4. Final Sprint Roadmap (Next Steps)

Next 10 hours. (1) Complete the user-started Python-3.11 isolated notebook run without altering its directory; (2) regenerate and compare the qualitative evidence tables; (3) add the resulting prediction-versus-truth plot only if its inputs and split are traceable; (4) freeze a code tag, environment lockfile, model artefact and submission CSV; and (5) rehearse the offline dashboard demonstration.

Refinement plan. First, replace per-descriptor agreement with chemically grouped attribution agreement and re-test fidelity. Second, run repeated group-aware calibration on scarce targets; release coverage only when it meets the declared tolerance. Third, pre-register a small external literature panel before seeing predictions and show all outcomes, including misses. Fourth, test additional Tg features tied to rigidity/free volume and accept them only if they improve grouped validation without weakening rewrite invariance.

Final output. The delivery will be (i) the reproducible notebook and pinned environment, (ii) the submission CSV and model artefact, (iii) evidence tables/figures with a claim-to-artifact map, (iv) a static report, and (v) an offline dashboard that shows a polymer structure, predicted property, interval, applicability tier, nearest analogue and feature-level explanation. The dashboard is a decision-support demonstration; it will distinguish its portable per-row model from the competition submission pipeline.

## References

- Kim, C. et al. Polymer Genome: A data-powered polymer informatics platform. J. Phys. Chem. C (2018). https://doi.org/10.1021/acs.jpcc.8b02913

- Grinsztajn, L., Oyallon, E. & Varoquaux, G. Why do tree-based models still outperform deep learning on typical tabular data? NeurIPS (2022). https://papers.nips.cc/paper_files/paper/2022/hash/0378c7692da36807bdec87ab043cdadc-Abstract.html

- Landrum, G. RDKit: Open-source cheminformatics. https://www.rdkit.org

- Rogers, D. & Hahn, M. Extended-connectivity fingerprints. J. Chem. Inf. Model. (2010). https://doi.org/10.1021/ci100050t

- Lundberg, S. M. & Lee, S.-I. A unified approach to interpreting model predictions. NeurIPS (2017). https://arxiv.org/abs/1705.07874

- Hooker, S. et al. A benchmark for interpretability methods in deep neural networks. NeurIPS (2019). https://arxiv.org/abs/1806.10758

- Angelopoulos, A. N. & Bates, S. A gentle introduction to conformal prediction and distribution-free uncertainty quantification (2021). https://arxiv.org/abs/2107.07511

- OECD. Guidance Document on the Validation of (Q)SAR Models (2007). https://www.oecd.org/env/guidance-document-on-the-validation-of-quantitative-structure-activity-relationship-q-sar-models-9789264085442-en.htm

- Krogh, A. & Vedelsby, J. Neural network ensembles, cross validation, and active learning. NeurIPS (1994). https://proceedings.neurips.cc/paper/1994/hash/b8c37e33defde51cf91e1e03e51657da-Abstract.html

- Fox, T. G. & Flory, P. J. Second-order transition temperatures and related properties of polystyrene. J. Appl. Phys. (1950). https://doi.org/10.1063/1.1699435

## Appendix A — reproducibility and release record

| Item | Location / release condition |
| --- | --- |
| Submitted pipeline and architecture | AISEHack-2.0-Sandman-Polymer-Property-Prediction-Codebase/ |
| Notebook release gate | fixes/isolated_runs/Sandman_Polymer_Property_Prediction_2_906.ipynb; user-started run is in progress and must validate before promotion |
| Claim-to-evidence audit | fixes/qualitative_evidence/claim_evidence_map.md |
| Public repository URL | [Insert final GitHub release URL/tag] |
| Environment | Python 3.11.7; export the completed isolated environment lock/requirements with the final tag |
| Related draft | Personal/Research_Paper/paper.md is a separate, in-preparation research draft; it is not evidence for this check-in and should not be cited as a published result. |

GenAI disclosure. Generative-AI tools assisted with code scaffolding, documentation and literature triage. Numerical claims in this report are retained only when linked to a project artifact; generated prose is not treated as experimental evidence.

## Appendix B — visual and claim manifest

| Suggested visual | Local file | Purpose |
| --- | --- | --- |
| Architecture | AISEHack-2.0-Sandman-Polymer-Property-Prediction-Codebase/outputs/architecture.png | required workflow/novelty figure |
| EDA novelty regimes | AISEHack-2.0-Sandman-Polymer-Property-Prediction-Codebase/outputs/eda/novelty_two_regimes.png | why target-specific lanes are needed |
| Verified qualitative figure | finals/assets/verified_qualitative_evidence.png | invariance, explanation stability, generalisation and applicability boundary |
| Prediction-versus-truth parity plot | fixes/isolated_runs/outputs/training/parity_plots.png | insert only after the active isolated run completes and is validated |
| Feature-removal fidelity | AISEHack-2.0-Sandman-Polymer-Property-Prediction-Codebase/outputs/explainability/fidelity_curve_tg.png | optional appendix evidence for explanation fidelity |

The rendering source for Figure 2 is finals/scripts/build_verified_qualitative_figure.py; it reads only the named archived evidence CSVs and intentionally omits unresolved uncertainty metrics.

We, team Sandman, have made our submissions wholly based on our own efforts and have not taken help from third parties / members not part of the team. (Confirm this declaration and the team name before submission.)